# Phase separation induced by hydration of the mixed Ca/Sr aluminates Ca3-xSrxAl2O6 - A crystallographic study

Author	Prodjosantoso A.K. · Kennedy B.J. · Hunter B.A.

Published	April 2002

#### Abstract

The compounds formed by the hydration of single-phase samples of the mixed, solid solution, Ca/Sr aluminates, Ca3-xSrxAl2O6, 3=<x=<0 have been studied using high-resolution synchrotron powder diffraction. Hydration of these mixed metal aluminates generally resulted in the formation of at least two hydrogarnet phases, one Ca-rich and the other Sr-rich. The structures of these hydrogarnets have been refined from neutron or synchrotron powder X-ray diffraction (XRD) data. A simple solubility model to explain the phase separation is presented.

Journal	Cement and Concrete Research